## Slide 1: Efficient inference of stochastic temperature fields with applications to laser powder bed fusion Ti6Al4V Vamsi Subraveti CE6310 Final Project Multiscale Computational Mechanics Laboratory Vanderbilt University
April 28, 2025

## Slide 2
Table of contents
Overview of LPBF and problem statement
Experimental data description
Model formulation
Calibration via particle filter
Uncertainty propagation
Extensions, limitations, and future work

## Slide 3
Background
Laser powder bed fusion (PBF-LB): metal additive manufacturing technique used to build complex, bespoke parts
Qualification and certification (Q+C) of these parts is an open challenge due to build/test cost
Model-based Q+C spearheading the effort to bring parts into production for aerospace
Process-structure property models need to account for uncertainties at each step in the process + how they aggregate
Problem focus: using melt pool data from experiments, infer underlying thermophysical parameters of a stochastic temperature field model
Process
Experiment
Model
In situ melt pool characterization
Flat plate characterization
Single track/ multi track characterization
Serial sectioning
Powder modeling
Thermal field model from laser – analytical, numerical
Heat transfer/fluid flow simulations
Ray tracing simulations
Spatter modeling
Defect modeling
Data flow
Structure
Property
Experiment
Experiment
Model
Model
X-ray crystallography on microstructures
Grain size, grain orientation distributions
Texture identification
Various types of fatigue testing
Runout
Cycles to failure
Fractography
Grain growth and solidification models
Kinetic Monte Carlo, phase field, CA
Texture / orientation models
Alloy composition models
Post-build treatment modeling
Mechanical models (multiscale, PINN, PUCM)
Fracture models
Data flow
Data flow
Measurement
error
Laser
parameters
Layer
thickness
Powder
composition
Thermophysical
properties
Experiment
Melt pool data
Model form
error
Calibration of thermal model
Stochastic temperature fields

## Slide 4
Experimental data, calibration idea
From collaborators at CMU, we have high-quality top-down melt pool width measurements at various processing parameters for Ti6Al4V
We can use the melt pool width (under symmetrical assumptions) to define the liquidus contour in a temperature field

## Slide 5
Model description: thermal field, width estimation
The Rosenthal model is a popular analytical heat source model that solves heat conduction for a moving point source
  Many simplifications are made (heat source, no fluid flow/phase change), so we will introduce model form error
Pribe et al. 2023 developed a quick numerical approximation of the width in a Rosenthal temperature field
  Approximately solves for width by finding roots of a nonlinear function via Brent’s method – a relative of secant method
For a point source in moving in the direction
Preheat temperature
Absorptivity
Thermal conductivity
Density
Specific heat
Power
Velocity
Distance from source in moving reference frame
X-coordinate in moving reference frame
Scan vector
Notes: Type equation here.
"Type equation here."

## Slide 6
Model description: particle filter
We will assume that thermal conductivity, absorptivity, density, and specific heat are stochastic
Let
Particle Filter algorithm ( particles, experimental observations)
  Solve for
  Initialize particles using OLS guess
  Initialize
  Initialize weight vector
  Repeat until
    Sample particles based on weight vector
    Initialize ; Repeat until
      Evaluate likelihood function
      Update weight
    Normalize weight vector
    Filter particles/weights based on pctile of weight
Initialization of particles around the OLS solution at t=0.

## Slide 7
Particle filter results
500 subsamples of N=30000 measurements of melt pool width evolution
500 particles propagated
50% of particles initialized around OLS soln. at
After each iteration, top 25% of particles were kept for importance resampling
Importance resampling of the top 25% of particles
75% of particles were initialized uniform random within reported experimental bounds of property
Time to run calibration with filter: 11.43s

## Slide 8
Propagation of parameter, model form uncertainty
Extracting optimal particle at each timestep, executing width model n=20 times to obtain variance in width estimation
Model mean, model variance extracted at each of 500 subsampled timesteps
Time to run inference with n=20: 9.49s
Model shows good response to large fluctuations in width
Variance increases with smaller fluctuations, possibly due to many near-optimal particles
  Filter would select against non-optimal particles in extreme fluctuation cases
  Many near-optimal particles could result in less accurate estimation of width

## Slide 9
Inferred stochastic temperature field

## Slide 10
Difference in temperature fields, optimal particle
Evaluated the model once with the optimal particle at each timestep and plotted the difference in temperature field relative to the OLS particle solution
  Does not account for overall model uncertainty
  Does show the difference in uncertain parameters (stochastic processes) vs. static parameters (constants)

## Slide 11
Future work
Calibrate model form error variance
  Will likely have to regularize via Tikhonov to ensure that error terms do not dominate fluctuation of parameters
Compute stochastic temperature field QoIs
  Time-varying thermal gradients
Extend to PSPP models
  Time-temperature histories can now include uncertainty in temperature field at various processing conditions
  This uncertainty could be propagated to grain nucleation/formation models, such as kinetic Monte Carlo, cellular automata, phase field
Develop stochastic optimal control problem for real time build optimization
  How to define control trajectories for P, V to minimize/maximize objective function with design constraints
  Example: Vary P with time to control width (or dWidth/dt) falling below a certain threshold
  Likely a multi-objective stochastic optimization problem
Extend with work in ORNL this summer (Coleman et al. 2024)
  Calibration of supergaussian dynamic heat source form in heat equation
  Simulation method: finite volume (OpenFOAM), will likely require surrogate
  Capture a range of melt pool cross sectional morphologies evolving in time